The Degradation of Lubricants in Gasoline Engines:

Part 1: A Combined Tribological, Rheological and Chemical Model for Lubrication Degradation in the Piston Ring Pack

(Abstract for STLE Conference, Toronto, May 2004)

Moray S. Stark*, John R. Lindsay Smith, Julian J. Wilkinson

# Department of Chemistry, University of York, York YO10 5DD, UK

Peter M. Lee, Martin Priest

# School of Mechanical Engineering, University of Leeds, Leeds, LS2 9JT, UK

R. Ian Taylor

# Shell Global Solutions, Shell Research Ltd, PO Box 1, Chester, CH1 3SH, UK

Simon Chung

# Infineum UK Limited, PO Box 1, Milton Hill, Abingdon, Oxfordshire, OX13 6BB, UK

The automotive industry requires lubricants that will have longer drain intervals and higher performance (such as lower component wear and increased fuel economy) and this must be achieved within ever tightening compositional constraints, for example, reduced phosphorus levels. To help the design of the next generation of lubricants, this project is studying the fundamental behaviour of lubricants in gasoline engines. A detailed tribological model of the oil flow in the piston ring pack has been constructed. This is combined with a detailed chemical model describing the oxidation of the hydrocarbon base fluid and a rheological model that describes how lubricant degradation products affect the viscosity of the oil. The predicted viscosity change of the lubricant during use feeds back into the tribological model to give a prediction of the change in performance of the lubricant in the engine as the oil degrades. This talk will discuss the progress made on this project, and experiments that have been done to verify the models.

# * Biography for Presenting Author

Moray Stark has a BSc and PhD in Physics, but has been working as a Chemist for longer than he can remember. The past few years have been spent specialising in the study of the oxidation mechanisms of hydrocarbon and ester lubricant base fluids, and the effects that oxidation products have on the rheology of lubricants. This work is sponsored by Shell Global Solutions (UK) and Infineum.